Specifications

The pole shall be constructed by the filament winding process to achieve optimum results for strength and rigidity. The filament winding process shall be continuously applied with uniform tension onto a rotating mandrel and shall result in a minimum mass glass to resin ratio of 70:30. The surface shall be seamless, smooth and tapered.

The material of the finishing coat shall be a gel coat that shall comply with the requirements of SANS 1749 and shall be applied to a uniform thickness of between 250 and 500 microns. It shall provide a weatherproof, UV resistant, flame resistant and impact strong surface in the colour specified.

A standard pole supporting a luminaire with a wind surface of 0.20m² shall not have a pole top deflection of more than 5% of its height above ground when subjected to a basic wind pressure of 500 Pa. A safety factor of 2.5 times the total maximum windload shall be applicable.

The pole shall be manufactured in accordance with SANS 1749 under the ISO 9002 quality system.

If an access opening is required, the cut-out shall be covered by an access door cover manufactured from glass filled nylon impregnated in the same colour as that of the surface coat. It shall be secured to the pole by two stainless steel Allen head captive screws into M4 brass inserts embedded in the pole.

A cable entry with a minimum diameter of 34mm shall be provided at a minimum depth of 400mm below the ground surface.

A hot dipped galvanised glandplate, suitable for gland no. 0 or 1, complete with terminal block and DIN rail for a miniature circuitbreaker, shall be provided and shall be mounted to a bolt provided in the access opening.

Poles for direct embedment in the ground shall be provided with a 300x300x1.6mm hot dipped galvanised baseplate complete with 2 x hot dipped galvanised steel hookbolts and nuts. Base mounted poles shall have a hot dipped galvanised flange plate that can be bolted to a foundation which shall be designed to withstand the forces the pole will experience in service.

| RELEVANT POLE DATA AND OTHER FACTORS | CORRESPONDING CALCULATED KEY VALUES |
| --- | --- |
| Total length of pole m | Height of pole above ground m | Diameter of pole at ground level mm | Load to be applied in pole-top deflection test N | Maximum permitted deflection in pole-top deflection test mm |
| 2.6 | 2.0 | 110 | 135.4 | 100 |
| 3.1 | 2.5 | 120 | 143.4 | 125 |
| 3.6 | 3.0 | 128 | 152.0 | 150 |
| 4.1 | 3.5 | 135 | 161.0 | 175 |
| 4.6 | 4.0 | 146 | 171.6 | 200 |
| 5.2 | 4.5 | 155 | 182.3 | 225 |
| 5.7 | 5.0 | 164 | 193.6 | 250 |
| 6.3 | 5.5 | 173 | 205.4 | 275 |
| 6.9 | 6.0 | 170 | 213.7 | 300 |
| 7.4 | 6.5 | 178 | 225.9 | 325 |
| 8.0 | 7.0 | 186 | 238.6 | 350 |
| 8.6 | 7.5 | 194 | 251.8 | 375 |
| 9.2 | 8.0 | 202 | 265.5 | 400 |
| 9.8 | 8.5 | 210 | 279.7 | 425 |
| 10.4 | 9.0 | 218 | 294.3 | 450 |
| 11.0 | 9.5 | 226 | 309.4 | 475 |
| 11.6 | 10.0 | 237 | 326.8 | 500 |
| 13.4 | 11.5 | 290 | 463.4 | 575 |
| 14.0 | 12.0 | 300 | 504.0 | 600 |

NOTES:

1. Relevant pole data is based on a shape factor of 0.7 and a calculated wind pressure of 500.14 Pa.

2. Corresponding calculated key values are based on a luminaire surface area of 0.2 m2 with a shape factor of 1.